GOVERNMENT OF ANDHRA PRADESH

EDUCATION (SSA) DEPARTMENT

From								To

Smt V.Usha Rani, I.A.S.,					The Project Officer,

State Project Director,					RVM(SSA) in the State.

Rajiv Vidya Mission (SSA),

Andhra Pradesh, Hyderabad.

Rc.No.512/RVM(SSA)/C4/2012, Dt:    .04.2013

Sub:- RVM(SSA, AP., Hyderabad – Supply of Uniforms for the year 2012-13 – Issue of Guidelines for procurement of uniforms – Clarification – Issued – Reg.

Ref:- 1. This office circular No.512/RVM(SSA)/C4/2012, Dt:17.11.2012.

2. G.O.Ms.No.24, Industries&Commerce(Tex)Dept., Dt:22.03.2013.

3. Clarifications sought by certain POs of RVM(SSA).

***

With reference to the clarification sought by certain Project Officers of RVM(SSA) in the State in the reference 3rd cited, I am to inform you that the specifications of the cloth was already communicated for procurement of Uniforms cloth to the students in their districts.

However the specifications of cloth is communicated for procurement of Uniform cloth from the Mills/Agencies other than APCO.  The specifications of cloth to be supplied by APCO will be communicated shortly.

Encl : Specifications							Yours faithfully

State Project Director

Rc.No.4582/A3/RVM(SSA)/2012, Dt:16.05.2013

True copy communicated to all the MEOs in the District with instructions to circulate the guidelines for specification for procurement of uniform cloth from the mills/agencies other than APCO to the students for the year 2012-13.  This copy communicated to all the SMC committees in your mandal without fail.

Project Officer,

Rajiv Vidya Misssion (SSA),

Prakasam District, ONGOLE.

To

All the Mandal Educational Officers in the District.

SPECIFICATIONS / PARAMETERS

Suiting Dyed.

| Sl.No. | Test Parameter | Requirement | Tolerance |
| --- | --- | --- | --- |
| 1 | Warp Count | 2/30s PC/PV | ± 5% |
| 2 | Weft Count | 2/30s PC/PV | ± 5% |
| 3 | Blend Composition (Ward & Weft) | 67:33 | ± 3 Units |
| 4 | Ends / Inchs. | 62 | + 5% - 2.5% |
| 5 | Picks / Inchs. | 46 | + 5% - 2.5% |
| 6 | Width | 137 Cms | ± 1 Cm |
| 7 | Length | 17 Mtrs.and above |  |
| 8 | Mass (GSM) | 190 grams | + 5% - 2.5% |
| 9 | Breaking Strength Warp | 90 Kgf | - 5% on average |
| 10 | Breaking Strength Weft | 65 Kgf | - 5% on average |
| 11 | Crease recovery angle | As per Standard IS 15853:2009 | As per Standard IS 15853:2009 |
| 12 | Pilling Resistance |  |  |
| 13 | P.H.Value (Hot method) |  |  |
| 14 | Colour Fastness to Light |  |  |
| 15 | Colour Fastness to washing Test 2 |  |  |
| 16 | Dry-cleaning |  |  |
| 17 | Colour Fastness to Perspiration |  |  |
| 18 | Colour Fastness to Rubbing |  |  |
| 19 | Colour Fastness to Hot Pressing |  |  |
| 20 | Tear Strength |  | As per Standard IS 15853:2009 |
| 21 | Drape, percent |  |  |

Shirting.

| Sl.No. | Test Parameter | Requirement | Tolerance |
| --- | --- | --- | --- |
| 1 | Warp Count | 2/60s PC/PV | ± 5% |
| 2 | Weft Count | 30s PC/PV | ± 5% |
| 3 | Blend Composition (Ward & Weft) | 67:33 | ± 3 Units |
| 4 | Ends / Inchs. | 64 | + 5% - 2.5% |
| 5 | Picks / Inchs. | 62 | + 5% - 2.5% |
| 6 | Width | 91/137 Cms | ± 1 Cm |
| 7 | Length | 17 Mtrs.and above |  |
| 8 | Mass (GSM) | 115 grams | + 5% - 2.5% |
| 9 | Breaking Strength Warp | 50 Kgf | - 5% on average |
| 10 | Breaking Strength Weft | 50 Kgf | - 5% on average |
| 11 | Crease recovery angle | As per Standard IS 15852:2009 | As per Standard IS 15852:2009 |
| 12 | Pilling Resistance |  |  |
| 13 | P.H.Value (Hot method) |  |  |
| 14 | Colour Fastness to Light |  |  |
| 15 | Colour Fastness to washing Test 2 |  |  |
| 16 | Colour Fastness to Perspiration |  |  |
| 17 | Colour Fastness to Rubbing |  |  |
| 18 | Colour Fastness to Hot Pressing |  |  |
| 19 | Tear Strength |  | As per Standard IS 15853:2009 |
| 20 | Abrasion resistance |  |  |