WELDING PROCEDURE SPECIFICATION

WPS -

2010-xxxx-23

REV. NO.:  2

DATE: 10/8/2009

**APPLICABILITY**

WELDING PROCESS:

GTAW-

and GTAW-

ASME: X

AWS: X

OTHER:

SUPPORTING PQR:

200-23-P	P-WS-10-1	P-WS-10-2	P-WS-151-1

P-WS-100-2	P-WS-100-1

2010-xxxx-23

JOINT:

This WPS shall be used in conjunction with the General Welding Standards (GWS) and Welding

Fabrication Procedure (WFP) sections and criteria for joint details, repairs, NDE, inspection etc.

Weld Joint Type:

Butt/Groove/Fillet

Class:

Full/Partial Penetration

See GWS 1-06 and WFP's for joint details	Preparation:

Thermal (plasma) /Mechanical

Root Opening:	0 - 3/32

Backing:

None/Strap/back welding

Backgrind root:

or purged

Backing Mat.:	Al

Bkgrd Method:	Grind if not purged

GTAW Flux: N/A	Backing Retainer:  N/A

FILLER METALS:

Class:

ER4043

and

ER4043

A No:

N/A

SFA Class:

5.10 and 5.10

F No:

23 and 23

Size:

1/16	3/32	1/8

Insert:

N/A

Insert Desc.:   N/A

Weld Metal Thickness Ranges:

Flux: Type:   NA

Size: 0

AWS Root Pass:	0.032

thru

0.75

| AWS Balance: | 0.032 | thru | 0.75 |
| --- | --- | --- | --- |
| ASME Root Pass: | 0.032 | thru | 0.187 |
| ASME Balance: | 0.064 | thru | 0.75 |

| AWS Balance: | 0.032 | thru | 0.75 |
| --- | --- | --- | --- |
| ASME Root Pass: | 0.032 | thru | 0.187 |
| ASME Balance: | 0.064 | thru | 0.75 |

Filler Metal Note:

BASE MATERIAL

P/S No.  23

Gr No.

All

to: P/S No.  23

Gr No. All

Spec.

B-209 Al- Plate & sheet

Grade: All

to: Spec.

B-209 Al- Plate & sheet

Grade: All

| Qualified Pipe Dia. Range: ≥ | AWS: | 6 | ASME: | 0.75 |  |
| --- | --- | --- | --- | --- | --- |
| Qualified Thickness Range: | AWS: | 0.032 | thru | 0.750 | ASME: | 0.032 | thru | 0.750 |

QUALIFIED POSITIONS:

AWS: All

ASME: All

Vert. Prog.:

V/Up

Preheat Min. Temp.:

70 °F

GAS: Shielding:

Argon	or

Interpass Max. Temp.:

500 °F

Gas Composition:

100   /	0

/	0	%

0 /	0 /	0 %

Preheat Maintenance:

70 °F

Gas Flow Rate cfh:

10	to	25

0  to	0

| PWHT: Time @ °F Temp. 0 |  | Backing Gas/Comp: |  | Argon | 100 % |
| --- | --- | --- | --- | --- | --- |
| Temp. Range: | 0 °F | Backing Gas Flow cfh: | 3 | to 10 |  |
| to | 0 °F | Trailing Gas/Comp: |  | N/A | 0 % |

APPROVAL:

Signatures on file at ENG

DATE:

10/8/2009

WPS NO:

2010-xxxx-23

WELDING CHARACTERISTICS:

Current:	AC

and   AC

Tungsten Type: EWTh-2

Transfer Mode: N/A

Ranges: Amps

Volts

25 to

12 to

300	Tungsten Dia.:	3/32

22

Pulsing Cycle: 40

Background Current: 40%

to  60

Fuel Gas:

N/A

Flame: N/A

Braze temp. °F 0

to  0

WELDING TECHNIQUE:

Technique:  Manual

For fabrication specific requirements such as fit-up, cleaning, grinding, PWHT and inspection criteria refer to Volume 2, Welding Fabrication Procedures

Cleaning Method:	Wire Brush, File, Grind

Single Pass or Multi Pass: GMAW Gun Angle °:

M

0  to  0

Stringer or Weave bead (S/W): S/W or

Forehand or Backhand for GMAW (F/B):

Oscillation:

N N/A

No Pass >1/2":

GMAW/FCAW Tube to work distance:	N/A

Maximum K/J Heat Input:  0

Travel speed: Variable

Gas Cup Size: # 5

PROCEDURE QUALIFIED FOR:

Charpy "V" Notch:

N/A

Nil-Ductil Transition Temperature: N/A

Dynamic Tear: N/A

Comments:

| Weld Layer | Manual Process | Filler Metals | Size | Amp Range | Volt Range | Travel/ipm | Nozzle Angle |  | Other |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | GTAW- | ER4043 | 1/16 | 25 | to | 160 | 12 | to | to | 0 to | 0 |
| 2 | GTAW- | ER4043 | 3/32 | 150 | to | 250 |  | to | to |  |  |
| 3 | GTAW- | ER4043 | 1/8 | 240 | to | 300 |  | to | to |  |  |
| 4 | GTAW- | ER4043 | 1/8 |  | to |  |  | to | to |  |  |

REM.

* Weld layers are representative only - actual number of passes and layer sequence may vary.