Suggested Items for Inspection & Test Plan

| Before Fabrication & Welding |  |
| --- | --- |
| Welding Machine Calibration | Annual calibration of welding machines. |
| Welding Machine Register | List type and location of welding machines and calibration data. |
| Verify Construction Code | AS 4100, AS 5100, AS 3990, AS 4600. |
| Check if dynamic/fatigue loading is to be considered. | Static, dynamic, fatigue or various types of wear. Use of quench and tempered material. |
| Verify Welding Code | AS 1554.1-7, AS 5131, AS 1210. |
| Obtain Material Test Certificate | Material Grade. Prequalified or to be qualified? Chemical analysis Tensile strength (MPa) Yield strength (MPa) Ductility (% elongation) Impact strength (Charpy) |
| Thick material | Check size, condition, heat numbers and mill certificate. Test for laminations, cracking and other defects. |
| Obtain Consumable Test Certificate | Check: classification, age/batch number, storage, conditioning. Prequalified or to be qualified? Chemical analysis Tensile strength (MPa) Yield strength (MPa) Ductility (% elongation) Impact strength (Charpy) Welding Shielding Gases (ppm. impurities). |
| All weld joints identified and numbered. | Fillets: single pass / multi-pass, weld size. Butts: type and thickness. Group joints via “Welding Code Joint ID Number.” Prequalified or to be qualified? |
| Positions for Welding | Number of welding positions required? |
| Allocate Welding Procedures to joints. | Weld map. |
| Prepare weld sequence map to minimize distortion. | Welding sequence and weld direction map. |
| Identify welds requiring NDT. | NDT method and weld length percentage. |
| Qualify welding operators | Welding Operator Performance Qualifications. |
| Maintain company Welding Register | No. of WPS’s, PQR’s and Qualified operators. |
| During Fabrication & Welding |  |
| Component - Mark out | Check material grade. Check dimensions. |
| Material cutting (mechanical) | Quality of cut edge. Removal of scale in weld area. Identification of off-cuts (material grade). |
| Material cutting (thermal cutting) | Check: Weld preparation dimension. Removal of scale in weld area. Identification of off-cuts (material grade). |
| Fit-up components | Check: dimensions, weld preparation, temporary attachment removal and material repair. Tack weld length (preheat if required) cleanliness of parts, fusible inserts, backing bar or strip where required. |
| Welding | Check: WPS No. in use. Verify preheat, amperage, arc voltage, shielding gas type and flow rate as per WPS. Root run in butts, back-grinding to clean metal, interpass temperatures, visual appearance, weld size, distortion. Cleaning between runs. Traceability of Welding Operators to specific welds. |
| After Fabrication & Welding |  |
| 100% Visual Scanning | Check that no welds have been missed and there are no obvious defects. |
| Non-Destructive Testing | Check Technician is min. Level 2. Witness NDT. |
| Weld Repairs | Check repair procedure, Witness repair, Witness NDT and confirm results. |
| Post Weld Heat Treatment | Verify type of heat treatment required. Witness heat treatment. Check temperature and times against code. Check heat treatment graph against code. |
| Prior to painting | Inspect: edges for radius, removal of spatter and flux, areas where temporary attachments are removed, protection of machined surfaces, surface cleaning and protection. |
| Grit blasting | Inspect: profile, surface protection. Check: environmental condition. |
| Painting | Witness: stages - records of humidity and material used. Inspect: thickness of coating, color match, uniform coating, transport damage, adhesion and “Holiday” tests of sample plates. |
| Assembly | Inspect: mechanical functional tests, lubrication, protection of surfaces, others as per engineering requirements. |
| Packing - dispatch | Witness: packing procedures, opening covers. Inspect: package identification, loading on transport. |
| Documentation | Prepare quality assurance documents. Manufacturer’s data report. Issue to specified person(s). Weld map. Welding Register. Material and consumable certificates. WPS’s, PQR’s, WOPQ’s, NDT Test Reports. ITP’s. File completed documents. |
| Non-Compliance | Document all repairs. |
| First Article Inspection | Customer to inspect and approve first article produced. |