Test of rubber TAN SS 09 from B. Reichard

This rubber I have found thankB.Reichard in 09/09

Static test was made at home during 2 minutes :

Size 1“/8 x 1“/24      cca  3,4 g/m      Test temperature  200C

Coefficient linear elastic  KL = 9,7  ( very good)

Hysterse    H0 = 12 %   poor

H30 = 5 %     -“-

H60 = 4 %     -“-

Nominal lap  Ln = (2x6,8)1/2   =  260 mm  for turns test : it brakes on 1120 turns

Km = 11,2   ( it is good , if it will be strong one)

Comparative flying tests made on my old float Peanut Sopwith RAINBOW which flies on a lap 1“/8

l = cca 300 mm or two laps 1“/16.  Turns max. this  lap new rubber is 1350 in 200C temperature.

Table of measuring in Královo Pole  station hall 23. 4. 2002   t= 170 C

| Rubber | weight /long | Turns max. | 70% Tmax. flight sec | 90%Tmaxflight. |
| --- | --- | --- | --- | --- |
| TAN II,FIN 3/95 strong | 2,4 g / 300mm | 1360 | 960 t, 45s | 1224 t., 59s |
| TANII,FIN 4/92 soft | 2,4 g / 300mm | 1410 | 1000 t, 40s | 1260 t., 52s |
| SIG II 2000 gray | 1,76 g / 330mm | 1320 | 912 t, 37s | 1188 t., 50s |

Table of measuring in Královo Pole  station hall  09/05 t= 250 C, 10/06 220C,  11/07100C

| Rubber | weight /long | Turnsmax | 65%Tmaxflight s. | 80%, s | cca 90%t, flight s |
| --- | --- | --- | --- | --- | --- |
| TANSS Rei/Hor 09/05 | 2,4 g / 300mm | 1550 | 960 t 35sec. | 1200t 45s | 1400 t., 60s |
| TANSS Horejsi 10/06 | 2,4 g / 300mm | 1410 | 900 t, 32s | 1280t 48s | 1350 t., 55s |
| TANSS Supply 10/06 | 2,3 g / 310mm | 1360 | 870 t, 24s | 1100t 29s | 1200 t., 32s |

Table of measuring in Královo Pole  rail station hall  10/04/09  t= 200 C

| Rubber | weight /long | Turnsmax | 65%Tmaxflight s. | 80%, s | cca 90%t, flight s |
| --- | --- | --- | --- | --- | --- |

TAN SS 08 received

| 04/09 from Woodhousse | 2,1 g / 316mm |
| --- | --- |

1500

1000 t.

15 sec.

1200 t .

20 s

1350 t.

24 s

Table of measuring in Královo Pole  rail station hall  08/09/09  t= 200 C

| TANSS Reich 09/09 | 2,3 g / 310mm | 1350 | 870 t, 25s | 1080t 29s | 1210 t., 41s |
| --- | --- | --- | --- | --- | --- |

The firtst flight was very good, peanut climbed to 3m high landed in few turns, flying time was OK.

The second fight was marked big hystereze, peanut climbed to 5 m high landed with many turns and flying time was poor.

The third fight was marked very big hystereze, peanut climbed to 6 m high landed with many turns and flying time was poor too.

Normally this peanut climbs nearly to the ceiling in 8,5m height on the best rubber. But flights on the new rubber were  lower to 6 m height only. The best time on this rubber is poor (only 65 % of the my best old rubber). This rubber is stronger and better in compare the very poor TAN SS 08. We can use it for our P-30 models (2 laps only), but it will give a lower times than the best rubber TAN SS 05. Similar will be using this new rubber for 1/20 scale class and for old-timers.

Brno , 8. 8.  09

Lubomir  Koutny

Test gumy TAN SS 09  od B. Reicharda

Tuto gumu jsem získal od B. Reicharda v 09/09

Statický test  byl hotový bìhem dvo minut a mùže si jej každý udìlat I pøímo v prodejnì

Rozmìry = 1“/8 x 1“/24      cca  3,4 g/m      Teplota 200C

Lineární prùtažnost   KL = 9,7  ( velmi dobrá)

Hysterze    H0 = 12 %   špatná

H30 = 5 %     -“-

H60 = 4 %     -“-

Nominalní smyèka  Ln = (2x6,8)1/2   =  260 mm  pro obrátkový test : strženo pøi tøetím natoèení 1120

Km = 11,2   (je to dobré, bude li guma tvrdší)

Komparativní letové testy dìlané tradiènì na plovákovém peanutu Sopwith RAINBOW, který létá na smyèku 1x3 mm

l = cca 310 mm .  Maximální otáèky této smyèky jsou 1350 pøi 200C .

Pøikládám I døívìjší testy rùzných gum pro porovnání:

Table of measuring in Královo Pole  station hall 23. 4. 2002   t= 170 C

| Rubber | weight /long | Turns max. | 70% Tmax. flight sec | 90%Tmaxflight. |
| --- | --- | --- | --- | --- |
| TAN II,FIN 3/95 strong | 2,4 g / 300mm | 1360 | 960 t, 45s | 1224 t., 59s |
| TANII,FIN 4/92 soft | 2,4 g / 300mm | 1410 | 1000 t, 40s | 1260 t., 52s |
| SIG II 2000 gray | 1,76 g / 330mm | 1320 | 912 t, 37s | 1188 t., 50s |

Table of measuring in Královo Pole  station hall  09/05 t= 250 C, 10/06 220C,  11/07100C

| Rubber | weight /long | Turnsmax | 65%Tmaxflight s. | 80%, s | cca 90%t, flight s |
| --- | --- | --- | --- | --- | --- |
| TANSS Rei/Hor 09/05 | 2,4 g / 300mm | 1550 | 960 t 35sec. | 1200t 45s | 1400 t., 60s |
| TANSS Horejsi 10/06 | 2,4 g / 300mm | 1410 | 900 t, 32s | 1280t 48s | 1350 t., 55s |
| TANSS Supply 10/06 | 2,3 g / 310mm | 1360 | 870 t, 24s | 1100t 29s | 1200 t., 32s |

Table of measuring in Královo Pole  rail station hall  10/04/09  t= 200 C

| Rubber | weight /long | Turnsmax | 65%Tmaxflight s. | 80%, s | cca 90%t, flight s |
| --- | --- | --- | --- | --- | --- |

TAN SS 08 received

| 04/09 from Woodhousse | 2,1 g / 316mm |
| --- | --- |

1500

1000 t.

15 sec.

1200 t .

20 s

1350 t.

24 s

Table of measuring in Královo Pole  rail station hall  08/09/09  t= 200 C

| TANSS Reich 09/09 | 2,3 g / 310mm | 1350 | 870 t, 25s | 1080t 29s | 1210 t., 41s |
| --- | --- | --- | --- | --- | --- |

První let na 65% byl velmi dobrý do výše 3m a pøistání s malým zbytkem otáèek.

Druhý let byl již poznamenán velkou hysterezí po prudkém výstupu v zatáèce 180 stupòù, následoval sestup do 1 m  a pak pomalý výstup do 5 m výšky, pøistání bylo s velkým zbytkem otáèek.

Podobnì i tøetí l let byl ještì více poznamenán velkou hysterezí po natoèení na doraz mìla guma velký moment a prudkém výstupu v zatáèce 180 stupòù, následoval opìt sestup do 1 m  a pak pomalý výstup do 6 m výšky, pøistání s velkým zbytkem.

Normálnì tento peanut na nejlepší gumu vystoupá až tìsnì pod strop do výšky 8,5 m. Bohužel na novou gumu byla výška jen 6 m. Snažil jsem se zamezit kosému pøemetu na zaèátku (sestupu v druhé polovinì prvního okruhu) zvìtšením negativu na vnìjším køídle, moc to nepomohlo. Test ukazuje mimoøádnì dobré èasy pøi prvním natoèení. Pak pøi dalších letech na stejný svazek jsou problémy s hysterezí. Pøi soutìžním létání lze toto øešit výmìnou svazku po každém letu.

Na závìr lze øíci, že tato guma je mnohem lepší než mizerné várky z let 2007 a 2008, ovšem dost zaostává za výbornou gumou TAN SS 2005.

Ing.Lubomír  Koutný

Brno , 8. 8.  09